Surface Roughness of Adherend vs. Strength

|  | Tensile Strength (psi) |
| --- | --- |
| File Roughness | Extra Fine | Fine | Medium | Coarse | Sand Blast |
| Adherend |  |
| Rigid PVC - Rigid PVC | 4830 | 4980 | 4830 | 4690 | 4980 |
| Copper - Copper | 4830 | 4980 | 4830 | 4690 | 5690 |
| Steel - Steel | 4410 | 4550 | 4410 | 4270 | 5120 |

Test Conditions

- Test specimen……………..  0.5 x 0.5 x 1.5 in

- Surface treatment…………  Polished with smooth-cut file and degreased with methyl chloroform

- Bonding atmosphere………  73.5˚F, 60% RH

- Curing time………………..  24 hours under above atmosphere

- Test instrument…………….  Strograph W-Type Tester

- Speed of load………………  20 mm (0.8in)/min

- Adhesive…………………...  Aron Alpha Type 201

- Test method………………..  ASTM D 2095