Open Time vs. Strength

|  | Tensile Strength (psi) |
| --- | --- |
| Open Time | Aron Alpha Type 201 | Aron Alpha Type 202 |
| 1 sec | 4980 | 4980 |
| 10 sec | 4980 | 4980 |
| 30 sec | 4830 | 4980 |
| 1 min | 3980 | 4830 |
| 3 min | 1850 | 2840 |
| 5 min | 1140 | 1850 |
| 10 min | 570 | 1000 |
| 15 min | 280 | 570 |

Test Conditions

A drop of the adhesive is placed on a surface of the test specimen for a specified time.  	Afterwards, the test specimen is bonded to the other surface.

- Test specimen……………..  Rigid PVC: 0.5 x 0.5 x 1.5 in

- Surface treatment…………  Polished with smooth-cut file and degreased with methyl chloroform

- Bonding atmosphere………  73.5˚F, 60% RH

- Curing time………………..  24 hours under above atmosphere

- Speed of load………………  20 mm (0.8in)/min

- Test method………………..  ASTM D 2095