Shelf Life (Storage Conditions vs. Strength)

| Temperature | Tensile Strength (psi) |
| --- | --- |
|  | Start | 1 month | 3 months | 6 months | 1 year |
| 41˚F (refrigerator) | 4980 | 4980 | 4980 | 4980 | 4980 |
| 68˚F | 4980 | 4980 | 4980 | 4980 | 3980 |
| 104˚F | 4980 | 4980 | 4980 | 4410 | 0 |

- 20g container in standard package was used for the shelf life test.

- Bonding speed change in storage shows a trend similar to that of tensile strength.

- When an inner bottle is opened, the pace of degradation will slightly increase.

- For the maximum shelf life, the adhesive should preferably be stored in a cool, dry and dark place.  Exposure to ultraviolet light should be avoided.

Test Conditions

- Test specimen……………..  Rigid PVC: 0.5 x 0.5 x 1.5 in

- Bonding atmosphere………  73.5˚F, 60% RH

- Curing Time………………  24 hours under above atmosphere

- Speed of load………………  20 mm (0.8in) /min.

- Adhesive…………………..  Aron Alpha Type 201, standard 20g

- Test Method………………..  ASTM D 2095