Vibration Resistance

|  | Initial Tightening Torque | Breakaway Torque |
| --- | --- | --- |
|  |  | Before Vibration | Vibration 105 Cycles |
|  | Lb-in | Lb-in | Lb-in |
| Aron Alpha Type 201 | - | 173 | 173 |
| Aron Alpha Type 102 | - | 304 | 304 |
| Without washer | 61 | 39 | 35 |
| Plain washer | 61 | 39 | 35 |

Test Conditions

- Adhesive………………….  Aron Alpha Type 201 & Type 102

- Test specimen……………..  M10 steel bolt and nut degreased with methyl chloroform

- Bonding method…………  Penetration

- Bonding atmosphere……..  73.5˚F, 60% RH

- Curing Time………………  24 hours under above atmosphere

- Measuring conditions………………..  NS High-speed Vibration-Machine

Amplitude…11 mm, Acceleration…20G,

Aggregate vibration…1,780 c/min.

Measured by Torque-meter

| Aron Alpha | Tensile Shear Strength |
| --- | --- |
|  | Under Normal Conditions | After Test |
|  | psi | psi |
| Type 101 | 3840 | 3840 |
| Type 201 | 3130 | 3130 |

Temperature Cycle Test

Test Conditions

- Temperature Cycle………..  (14˚F/2 hr.  Room Temperature/5 min)

- (104˚F/2 hr.  Room Temperature/5 min)

- Adherend………………….  Steel/Steel

- Test specimen……………..  Metal: 0.064 x 1.0 x 4.0  in

- Surface treatment…………  Sandblasted and degreased with acetone

- Measurements……………  Made after leaving the test specimens for 24 hours at 73.5˚F, 60% RH

- Speed of load………………  20 mm (0.8in)/min

- Test method………………..  ASTM D 1002

Note:  Bonding strength decreased when the steel test specimen was immersed in water or hydrochloric acid.  This appears to be due to the rusting of the specimen.  Also the decrease in bonding strength was observed when the test specimen was immersed in sodium hydroxide solution.  Both corrosion of the adhesive polymer and rusting of the test specimen appear to account for the decrease.

# Text boxes

x 3 Cycles